CRAWFORD COUNTY DEPARTMENT

OF  ENVIRONMENT HEALTH

111 E. Forest, Suite M   -   Girard, KS 66743

(620) 724-7088           FAX: (620) 724-7178

crawfordcountykansas.org

PROCEDURE TO PLUG BORE HOLES USED FOR WASTEWATER DISPOSAL

- Determine the total depth of the hole and then determine the depth to the bottom of the casing or bore hole where it encounters the old mine works.  If possible determine the length of the casing.  Record the diameter of the hole.

- Remove casing if possible.

- Place a packer or plug of some type at the bottom of the bored hole.  If this is not possible then rock or some type of fill will have to be dumped into the hole until the material has reached the bottom of the bore hole.

- Grout should be pumped to the hole by a tremie tube placed in a few feet off the bottom of the hole.  Grout should be of 60% neat cement, 40% fly ash.  Neat Cement is mixed at a ratio of one 94 pound bag of cement to 5 gallons of water.  The grout should fill the hole up to 3 feet of the surface.  At this point if the casing has not been removed it should be cut off.  The remaining hole should then be filled with a mixture of clay, bentonite and dirt and should be mounded slightly to allow for settling.

- A wwc-5 Form must be filled out for each bore hole.  The form must be returned to the Crawford County Environmental Department.  Address is listed  at the top.